Quantitative Structural Health Monitoring by Ultrasonic Guided Waves
Ankit Srivastava and Francesco Lanza di Scalea 

NDE & Structural Health Monitoring Laboratory, 
Department of Structural Engineering 
University of California, San Diego, La Jolla, CA 92093-0085, USA
Phone: +1-858-8221458. E-mail: ansrivas@ucsd.edu and flanza@ucsd.edu
[image: image1.png]i " Mono-dimensional
Element

Q
U \: \UW

Z1 Ux
L2 AN
U v Uy2
Ux3
7

O
UZB\I/ e Uy3




Ankit Srivastava is a doctoral student in the Department of Structural                                                                                                                               Engineering at the University of California, San Diego (UCSD). He obtained his Bachelor of Technology (B. Tech.) in Civil Engineering from the Indian Institute of Technology, Guwahati, India in 2004. He received his Master’s degree in Structural Engineering from UCSD in 2006 and is now continuing for a Ph.D. in the same department.
[image: image127.jpg]


Francesco Lanza di Scalea is a Professor in the Department of Structural Engineering of the University of California, San Diego (UCSD). He obtained his Laurea (summa cum laude) and doctorate degrees in mechanical engineering from the University of Palermo, Italy. He was a Fulbright Scholar at Michigan State University, from which he received a Master’s degree in Engineering Mechanics. He was then a Postdoctoral Fellow at the Johns Hopkins University prior to joining UCSD in 1999. He received the ASNT Faculty Grant Award in 2003, the ASNT Fellowship Awards in 2002 and 2006, the UCSD’s Hellman Faculty Fellowship Award in 2000 and 2002, and the Structural Health Monitoring “Person of the Year” Award in 2007. 
ABSTRACT

This paper will present a Global-Local (GL) method to simulate the interaction of ultrasonic guided waves with structural defects in plate-like structures. The GL method uses a full Finite Element (FE) discretization of the defected region to properly represent wave diffraction phenomena, and a suitable set of wave functions to simulate regions away from the joint. Displacement and stress continuity conditions are imposed at the boundary between the global and the local regions. The radiated wave field can be then calculated by using standard techniques (least squares method). The novelty of the proposed approach over previous GL techniques is the use of Semi-Analytical Finite Element (SAFE) modeling for the "global" simulation and the use of this technique to quantify defects by guided waves. The SAFE method, which only requires the discretization of the waveguide's cross-section, allows handling complex structures (e.g. multilayered composites, arbitrary cross-sections, etc.) in a computationally efficient manner. Applications of the GL method to damage quantification will be shown for the cases of notches in aluminum plates and delamination-like defects in aircraft composite panels. 

1. INTRODUCTION
Effective Structural Health Monitoring (SHM) techniques able to detect, locate and quantify damage are needed to ensure the proper performance and mission readiness of current and future aircrafts, as well as to minimize maintenance costs by taking appropriate remedial actions in a timely manner [1].  

Among the many SHM methods available, those based on guided stress waves are particularly suitable for probing components with waveguide geometries, such as the skin panels of aircraft fuselage and wings. It is known that guided waves can achieve larger monitoring ranges compared to “local” NDT methods (~meters instead of ~centimeters). At the same time, guided waves retain higher sensitivity to damage compared to “global” methods, such as modal analysis, because of the higher probing frequencies (~kilohertz versus ~Hertz). When guided waves pass through a defected region, complex scattering takes place. By studying the characteristics of the reflected and transmitted waves, quantitative information on the defects can be obtained.
Quantitative defect information can be extracted by using a hybrid formulation wherein the finite element method is used to model small regions near the defect whereas regions away from the defect are modeled using a suitable set of wave functions. Reference [2] developed a global-local finite element formulation for modeling axisymmetric scattering of a steady, compressive, incident elastic wave in a homogeneous, isotropic host medium with an axisymmetric inclusion. The hybrid method was also used in references [3, 4] to model defects in a plate and a cylinder, respectively. In the area of SHM of aircraft components, the method has been applied to model wave interaction with defected lap-shear joints [5], as well as notches and rivet-hole cracks in plates [6, 7]. Doyle (references [8, 9]) employed a similar global-local scheme wherein the global field was modeled by using spectral elements.
Many aircraft components are complex in either their geometry (e.g. multilayers, tapered thickness, etc.) or their material properties (e.g. anisotropic).  In this case theoretical wave solutions for the global portion are either nonexistent or hard to determine. The Semi Analytical Finite Element (SAFE) method can help handle these cases because of its ability to extract modal solutions of complex structures in a computationally efficient manner [10-17]. Reference [18] demonstrated the application of the hybrid formulation to the detection of holes in aluminum plates. The present paper extends the global-local approach to model notches in aluminum plates and delamination-like defects in composite panels.
2. THEORY
The geometry of the problem at hand is depicted in Figure 1 where the material inside the bounded surface has properties different from the outside due to the presence of local irregularities as a defect.

[image: image128.png]



Figure 1: Geometry of a general wave scattering problem by global-local method.
In order to best illustrate the hybrid method, assume that a plane time-harmonic wave is incident on the FEM boundary in Figure 1. The region inside the boundary is meshed and analyzed using standard finite element analysis; the region outside the boundary is represented by the linear combination of a set of global wave functions, here calculated from the SAFE method. The continuity of displacements and tractions on the mesh boundary must be satisfied through proper choice of the amplitudes of the wave functions.

2.1 Semi-Analytical Finite Element Method 

The SAFE method is employed to calculate the guided wave modeshapes Φ and eigenvalues ξ for any infinitely-uniform cross-section. These modeshapes and eigenvalues are used to calculate the forces and displacements on the boundary separating the Global from the Local region. In the SAFE method, at each frequency ω a discrete number of guided modes is obtained. For the given frequency, each mode is characterized by a wavenumber, ξ, and by a displacement distribution over the cross-section. For a Cartesian reference system, the waveguide cross-section is set in the y-z plane while the x-axis is parallel to the waveguide length (see Figure 2). 

[image: image129.emf]Defect

Incident wave

Reflected waves

Transmitted waves

LOCAL (FEM)

GLOBAL (SAFE)

GLOBAL (SAFE)


Figure 2: Waveguide cross-section in Cartesian coordinates for SAFE.
Subdividing the cross-section via finite elements, the approximated displacement at a point, 
[image: image2.wmf](,,,)

uuxyzt

=

, is given as:




[image: image4.wmf]()

eixt

uNUe

xw

-

=


where  
[image: image5.wmf](,)

NNyz

=

[image: image8.png]


 is the matrix of the shape functions,  is the nodal displacement vector for the e-th element, t is the time variable and i the imaginary unit. It can be noted that the displacement is described by the product of an approximated finite element field over the waveguide cross-section with exact time harmonic functions, 
[image: image9.wmf]()

ixt

e

xw

-

, in the propagation direction, x. The compatibility and constitutive equations can be written in synthetic matrix forms as:




[image: image11.wmf]Du

e

=



[image: image12.wmf]*

C

se

=


where  
[image: image13.wmf]e

 and  
[image: image14.wmf]s

 are the strain and stress vectors respectively,  D is the compatibility operator and  
[image: image15.wmf]*

C

 is the stiffness tensor which is general can be complex (viscoelastic behavior). More details on the compatibility operator can be found in Refs. [8, 9]. The principle of virtual work with the compatibility and constitutive laws, Eqs.(1) and (2), leads to the following energy balance equation 



where  [image: image19.png]


 is the waveguide cross-section area, [image: image21.png]


 is the waveguide volume, 
[image: image22.wmf]t

is the external traction vector and the overdot means time derivative. The finite element procedure reduces Eq.(3) to the set of algebraic equations:



[image: image23.wmf][

]

2

M

ABp

x

-F=


where the subscript 2M indicates the dimension of the problem with M the number of total degrees of freedom of the cross-sectional mesh. Details on the complex matrices A and B can be found in Ref. [11]. By setting  
[image: image24.wmf]0

p

=

 in Eq.(4), the associated eigenvalue problem can be solved as  ξ(ω) which gives the wavenumbers for the different Lamb modes of the structure at frequency ω. For each frequency ω, 2M complex eigenvalues ξm and 2M complex eigenvectors Φm are obtained. The solution is symmetric, i.e. for each pair (ξm, Φm), representing a forward guided mode, a pair exists representing the corresponding backforward mode [9]. The first M components of Φm describe the cross-sectional mode shapes of the m-th mode. Once ξm is known, the dispersion curves can be easily computed. The phase velocity can be evaluated by the expression 
[image: image25.wmf]/

phreal

c

wx

=

, where 
[image: image26.wmf]real

x

 is the real part of the wavenumber. The imaginary part of the wavenumber is the attenuation, att=
[image: image27.wmf]imag

x

, in Nepers per meter. 

2.2 Global-Local Method
The global functions, represented by Φn, are the displacements which satisfy the governing equations in the absence of the discontinuity.

The displacements at the mesh boundary are written as a sum of the contribution due to the incident wave and that due to the scattered waves. This displacement is then further used to satisfy the continuity conditions at the boundary.

The displacements at the left boundary are written as:


[image: image28.wmf]lincidentscattered

uuu

=+




[image: image30.wmf](

)

(

)

1

inj

L

ixix

ininjj

j

AeAe

xx

+---

--

+--

=

F+F

å



[image: image31.wmf](

)

in

ix

linin

uAeGD

x

+-

-

+--

éùéù

=F+

ëûëû


where the time-harmonic dependence is implicit.
Reference [4] gives a detailed description of matrices 
[image: image33.wmf],

GD

--

éùéù

ëûëû


. In essence,  is a matrix consisting of the modeshapes of the scattered modes whereas 
[image: image36.wmf]D

-

éù

ëû

 is a column vector which contains the resultant displacement due to these modes on the left boundary.
In equations (5a, 5b), Φ+ represents the modeshape of the incident waves travelling to the right, Φ- represents the modeshapes of the reflected waves travelling to the left; 
[image: image37.wmf]in

A


, 
, and 
 represent the amplitude, modeshape and wavenumber of the incident wave respectively;  represents the unknown amplitude of the reflected waves; superscript ‘+’ represents a wave travelling in the right and a superscript ‘-‘ represents a wave travelling in the left direction; x- represents the absolute value of the distance of the left boundary from the center of the meshed region; L is the total number of modes considered. In the same way, the displacements at the right boundary are written as:




[image: image47.wmf](

)

(

)

1

inj

L

ixix

ininjj

j

AeAe

xx

++++

+++

=

F+F

å



[image: image48.wmf](

)

in

ix

rinin

uAeGD

x

++

+++

éùéù

=F+

ëûëû


In equations (6a)-(6b), 
[image: image50.wmf]j

A

+

 represents the unknown amplitude of the transmitted waves and x+ represents the absolute value of the distance of the right boundary from the center of the meshed region.
The forces at the boundaries can be calculated by computing the consistent nodal force vectors due to displacements (5b) and (6b). The nodal forces at the left boundary are:

[image: image52.wmf]()

in

ix

linin

fAFeFD

x

+-

-

+--

éùéù

=-+

ëûëû


Fj is the consistent nodal force vector calculated from the displacement vector Φj. The nodal forces at the right boundary are:


[image: image54.wmf]()

in

ix

rinin

fAFeFD

x

++

+++

éùéù

=-+

ëûëû


2.3 Finite Element Model for Local Region
The conventional discretization process in the finite element method yields:



[image: image56.wmf]{

}

[

]

{

}

{

}

{

}

**

0

BB

qSqqP

dd

-=



[image: image57.wmf][

]

[

]

[

]

2

IIIB

BIBB

SS

SKM

SS

w

éù

=-=

êú

ëû



[image: image59.wmf]{

}

{

}

{

}

TTT

IB

qqq

=


Here, 
[image: image60.wmf][

]

K


, and 
 are global stiffness and mass matrices respectively; ω is the harmonic frequency; 
 and  are the nodal displacement vectors corresponding to interior and boundary nodes respectively; 
[image: image67.wmf]{

}

B

P

 is the interaction force vector at the boundary nodes; and 
[image: image68.wmf]{

}

*

q

 denotes complex conjugate of 
[image: image69.wmf]{

}

q

[image: image72.png][s]



. Forces on the boundary nodes due to the entire FE region, when displacement is imposed only on the boundaries, can be calculated by performing static condensation on  such that:

[image: image73.wmf][

]

[

]

[

]

[

]

1

*

BBBBBIIIIB

SSSSS

-

éù

=-

ëû


2.4 Global Solution
The nodal forces on the boundary due to displacements (5b) and (5b), as contributed from the FE portion, are:


[image: image74.wmf]{

}

{

}

*

l

FEM

boundaryBB

r

u

fS

u

ìü

ïï

éù

=

íý

ëû

ïï

îþ


For traction continuity, from equations (5), (6), and (11):

[image: image76.wmf]{

}

{

}

{

}

{

}

*

ll

FEM

boundaryBB

rr

fu

fS

fu

ìüìü

ïïïï

éù

==

íýíý

ëû

ïïïï

îþîþ


Rearranging the terms, the following final equation is obtained:


[image: image78.wmf][

]

[

]

(

)

{

}

{

}

{

}

**

BB

BBinBBin

SGFDPSq

éùéù

-=-

ëûëû





[image: image80.wmf]{

}

(

)

(

)

in

in

ix

inin

B

in

ix

inin

AFe

P

AFe

x

x

-

+

-

+

+

ìü

ïï

=

íý

ïï

îþ





[image: image82.wmf]{

}

(

)

(

)

in

in

ix

inin

B

in

ix

inin

Ae

q

Ae

x

x

-

+

-

+

+

ìü

F

ïï

=

íý

ïï

F

îþ





[image: image84.wmf]{

}

{

}

{

}

TT

T

DDD

-+

=





[image: image86.wmf][

]

0

0

F

F

F

-

+

éù

éù

ëû

êú

=

êú

éù

ëû

ëû





[image: image88.wmf][

]

0

0

G

G

G

-

+

éù

éù

ëû

êú

=

êú

éù

ëû

ëû


Equation (13a) is solved using least squares to calculate the coefficients 
[image: image90.wmf]j

A

-


, and 
. Reflection coefficients (
) and transmission coefficients () (due to the ith incident mode) are defined below:

[image: image98.wmf]j

ij

i

A

R

A

-

=



[image: image100.wmf];,

j

ij

i

A

Tji

A

+

=¹



[image: image102.wmf]1;

j

i

A

ji

A

+

+=


2.5 Energy Conservation

Energies are carried only by the propagating modes, which include incident, reflected and transmitted modes. The time averaged values of energy flux associated with the jth reflected and transmitted modes through the cross-section is given by:

[image: image103.wmf]2

2

ijiijj

IAR

wa

-

=



[image: image105.wmf]2

2

ijiijj

IAT

wa

+

=


where 

[image: image106.wmf]0

h

jjj

Fqzdz

a

+

éù

=

êú

ëû

ò


is the participation factor for the jth propagating mode and the integration is carried over the thickness of the plate (h).

3. RESULTS

3.1 Reflection for Notched Aluminum Plate
This study examined a semi-infinite plate with a notch defect. The plate modeled was aluminum, 1.58 mm (1/16 in) in thickness. The first notch considered was 0.16 mm in width and 0.32 mm in depth (Figure 3a). A finite region surrounding the notch (local domain) was discretized by rectangular, four-node finite elements. A total of ten elements were used in the thickness of the plate, and the mesh was kept uniform throughout the local domain. SAFE was used for the global domain. The zero-order symmetric mode, S0, was considered as the incident mode.

The results are shown in the plot of Figure 3a in terms of reflected energy relative to the incident, unit energy. As expected, the notch causes S0-A0 mode conversion since it breaks the symmetry of the waveguide. As a check for the accuracy of the analysis, energy conservation is preserved as the reflected S0 and A0 energies sum to the incident S0 energy. Mode conversion is found more pronounced at particular frequency values, namely 500 kHz, 730 kHz, 880 kHz and 950 kHz. 

A more shallow discontinuity was examined next. This was a notch extending 1.6 mm in width and 0.16 mm in depth, which more closely represented corrosion damage (Figure 3b). It can be seen that the resulting reflection spectra are different for the two defect cases. This suggests the potential for quantitative, rather than qualitative defect detection.
[image: image108.png]& . |_so,incdent SAFE 2-DFE
s n:""‘*?‘\_‘VT"VVJ Y, {Global) {local)

; .  So,reflected 3.2mm 3 6mm*.32mmnotch
T Aoreiected = 1] 1o
E ol 2 _ 16mm

zo o AN S/ So, incident

1.6mm* 32mm notch





Figure 3: Results of S0 wave scattering from defects in a plate from global-local models. (a) Energy spectra of reflected S0 and A0 (mode conversion) from sharp notch; (b) Energy spectra of reflected S0 and A0 (mode conversion) from shallow notch. 
3.2 Reflection and Transmission for Notched Aluminum Plate
In this case the global-local method was used to predict the scattered field in both reflection and transmission. The plate modeled was aluminum, 1.6 mm in thickness with a half thickness notch in the middle. Transmitted and reflected S0 and A0 modes were computed for an incident S0 mode. Energy conservation was again checked to test the validity of the method (Fig. 4). 
[image: image109.png]SAFE Global 2-D FE local SAFE Global
! ‘ 2*0.8 mm hole )

Soincident ¥— 7 mm — / So transmitted

—_— .
1.6 mm
D E— v
Soreflected. 16 mm » Ao transmitted

Ao reflected

12

So incident

-

o
®

Wansmitted
—

So reflected Ao reflecte
—— t>mu><t

100 200 300 400 500 600 700 800 900 1000

Frequency kHz

©
>

o
N

o

Normalized Energy
&





Figure 4: Results of S0 wave scattering from notch in a plate from global-local model in transmission.
3.3 Reflection and Transmission for Layered Composite
This example examined reflection and transmission in the more complex case of a layered composite plate. The plate modeled was a 1mm thick composite consisting of 8 layers of unidirectional carbon-epoxy laminae in a stacking sequence of [0/+45/-45/0]S. Material damping was ignored in the present study. A defect of length 3mm, consisting of the removal of certain layers, was introduced at various locations across the cross-section of the plate (Fig. 5). Global-local was used to predict the scattered fields for each case. The material density of each lamina is ρ=1530 kg/m3 and the elastic properties in the principal direction of material symmetry are given in Table 1, where 1 is the fiber direction, 2 is the direction perpendicular to the fibers in the laminate plane, and 3 is the through-thickness direction. For waves propagating along a direction ‘x’ oriented at any angle θ with respect to the fiber direction, 1, the SAFE model simply requires the rotation of the stiffness matrix of each lamina through



[image: image110.wmf]1

12

CRCR

q

-

=


where [image: image112.png]


 is the stiffness matrix in the lamina’s principal direction, and R1 and R2 are the rotation matrices

[image: image114.png]



[image: image115.png]



with m=cos(θ) and n=sin(θ). The governing eigenvalue problem of SAFE is then solved by using the rotated stiffness matrix in the constitutive relations.

	C11
	C12
	C13
	C22
	C23
	C33
	C44
	C55
	C66

	135
	5.7
	5.7
	14.2
	8.51
	14.2
	2.87
	4.55
	4.55


Table 1: Elastic properties (GPa) for the CFRP lamina.
[image: image116.png]'
N

=]

B0 1 m—

] > -

£ o . / SAFE Global
5 06 Sotransmitted  sq incident Soincident
@ . —

N o4 Ao transmitted So reflected -
g 02 So reflected L Ao reflected Aoreflected
S

o

2

N
(=]

120 220 320 420 520 620

Frequency kHz

1.2
>
gl
2 os s o SAFE Global
Bos otransmitted ¢/ ;ncident Soincident
N oa Soreflected -
202 So reflected Ao reflected
S
[« LY
2 20 120 220 320 420 520 620

Frequency kHz

1.2
>
%D 1 S — \\/
o8 So incident SAFE Global
g ° Sotransmitte Ao reflected o
.N o4 Sg reflected Soreflected -
go.z Ao reflected
S — = |
<) 0
2 20 120 220 320 420 520 620

Frequency kHz

2-D FE local

SAFE Global
3 mm wide defect
»1'mm .
10 mm “
So transmitted
Ao transmitted
2-DFElocal  safE Global
3 mm wide defect
l'mm .
10 mm 3
So transmitted
Ao transmitted
2-DFElocal  gAFE Global
/3 mm W|de defect
1 mm
10 mm -

So transmitted
Ao transmitted





Figure 5:  Results of S0 wave scattering from defects in a composite plate. (a) removal of top 2 layers; (b) removal of central 2 layers; (c) removal of top four layers.

Figure 5 shows the scattered fields for an So incidence over the defected layered composites. Three different defects are considered. Scattered fields from the removal of the top 2 layers (Fig. 5a) are compared to the removal of the middle two layers (Fig. 5b), and the removal of the top four layers (Fig 5c). 

It can be seen that the reflection strength increases as the defect is moved from the top of the plate (Fig. 5a) to the center of the plate (Fig. 5b). This can be explained by the energy distribution in the fundamental symmetric mode over the cross-section of the plate. Figure 6 plots the Poynting vector for the S0 mode at the frequency of ~400kHz across the cross-section of the composite plate. Poynting vector is the average power flow carried by a mode over a unit period of time, mathematically given as:

[image: image117.wmf](

)

*

1

Re

2

Pu

s

=-

&

 
where [image: image119.png]


 is the classical 3
[image: image120.wmf]´

3 stress tensor, and [image: image122.png]


 is the complex conjugate of the particle velocity vector.
[image: image123.png]Magritude of Poynting Vector

n
x10

12

() WBion ol

=
s

02

"
%10




Figure 6: Poynting Vector for S0 at 400 kHz in the CFRP laminate.

Figure 6 shows that the energy carried by the S0 mode in the direction of propagation is concentrated more around the center of the cross-section of the plate than at its surface. Therefore, it is expected that this mode would be more sensitive to a central defect compared to a defect at the top or the bottom of the plate. Figures 5a and 5b accordingly show an increased reflection of the S0 mode for the case when the middle 2 layers are removed as compared to the case when the top 2 layers are removed. In addition, mode conversion is completely absent in Fig. 5b given the symmetry of the defect with respect to the cross-section; alternatively, considerable mode conversion of S0 into A0 is seen in Fig. 5c because the defect breaks the symmetry of the cross-section. As expected, global-local predicts a significant increase in scattering as the defect size increases from 2 layer thicknesses to 4 layer thicknesses (Fig. 5c).
A0 incidence was studied for the same composite plate using the global-local method. Figure 7 shows the scattered fields for the same. As in the previous problem, three different defects are considered (Fig. 7 a-c).
Fig. 8 shows the magnitude of the Poynting vector for the fundamental anti-symmetric mode at 540 kHz. Similar to the case of S0, a very large part of the energy in the A0 mode is concentrated in the central portion of the plate’s cross-section. This explains the strong scattering from the central defect (Fig. 7b) compared to the top defect (Fig. 7a).

[image: image124.png]1.2

08

0.6

04

0.2

Normalized Energy

e © o o e
N R D RN

Normalized Energy

N~ o
. Ao incident
Aotransmitted 0 o ed

Ao reflected

So transmitted

20 120 220 320 420 520 620

Frequency kHz

20 120 220 320 420 520 620

e ° o ©° -
N & O ® = N

Normalized Energy

Frequency kHz

‘Ao transmitted

So transmitted
Ao reflected
rex

20 120 220 320 420 520 620

Frequency kHz

SAFE Global
Ao incident

So reflected -
Aoreflected

SAFE Global
Aoincident

So reflected -
Aoreflected

SAFE Global
Aoincident

So reflécted -
Aoreflected

2-D FE local  gAfE Global
-3 mm wide defect
}1:mm .
10 mm .
So transmitted
Ao transmitted
2-D FE local  gafg Global
,3mm wide defect
Amm
10 mm °
So transmitted
Ao transmitted
2-D FE local gaAfFg Global
,3mm wide defect
Tmm—
10 mm ‘

So transmitted
Ao transmitted





Figure 7:  Results of A0 wave scattering from defects in a composite plate. (a) removal of top 2 layers; (b) removal of central 2 layers; (c) removal of top four layers.
[image: image125.png]Magritude of Poynting Vector

n
x10

24 26 28 32
10"

22

12

() WBion ol

=
s

02





Figure 8: Poynting Vector for A0 at 540 kHz in the CFRP laminate.

3.4 Time Histories 

The global-local method was also used to predict the time-domain waveforms in an aluminum plate subjected to broadband, pulsed laser excitation. The response was experimentally measured for the case of a plate 1.58 mm in thickness with a sensor-excitation distance of 20 cm. Figure 9(a) shows the geometry of the problem. Figures 9(b) and 9(c) show the comparison of the theoretical predictions with experimentally measured results.

The numerical predictions were calculated by inverting the frequency response calculated from the SAFE-based global-local method. 
[image: image126.png]Laser Shot 5 mm wide, half thickness hole

Jem,/ = PICO Sensor
U ! 1/16inches

20cm

5 o | ndamaged T

B osl h / ged| 2 ndamaged
%_0.4- { ) I a

£ o2l E

< <

o] 0F e

‘_é"’"‘ Damaged g

595 Experimental & ] Damaged
2 o8| 2

0 2 r 6 8 10 12 10 12

Time (s) x10°





Figure 9: (a) Geometry of the problem; (b) Experimental measurements; (c) Numerical predictions
It can be seen that a small discrepancy exists between the model and the experiment in the wave arrival time of S0, whereas good match is found for A0. The S0 discrepancy may be due to an imperfect knowledge of the material in the test. It is nevertheless worth noting that both the numerical predictions and the experimental results show a decrease in the amplitude of the A0 mode in the case of the notched plate. The numerical prediction also shows significantly more mode conversion when compared to the experimental results. This is primarily because of energy conservation concerns for the plain strain approximation of a three dimensional problem. While energy is allowed to scatter in random directions in the experimental case, reducing the problem to 2 dimensions forces the scattered energy from the A0 mode to be transferred to the S0 mode. Further studies, including adding higher-order scattered modes, refining the finite element mesh, and extending the 2-D global-local formulation to 3-D, are being conducted to obtain a better convergence of the model with the experiments.
4. CONCLUSIONS

This paper demonstrates the use of SAFE in a global-local framework which allows extracting information on guided waves scattered by defects in plates for quantitative, rather than qualitative structural health monitoring. The advantage of SAFE is its ability to handle complex geometries or layered composites in a computationally efficient manner. 
The global-local method was used in a simple case of corrosion defects in aluminum plates and delamination-like defects in layered composites. Both reflected and transmitted spectra of guided waves were successfully predicted. It was also shown that the wave time histories can be extracted from these models. The proposed global-local formulation is being applied to other structural health monitoring applications, particularly to 3-D cases of adhesive bond defects in composite aircraft panels. 
5. ACKNOWLEDGMENTS
This project was funded by Air Force Office of Scientific Research contract no. FA9550-07-1-0016 (Dr. Victor Giurgiutiu, Program Manager) and by the Los Alamos/UCSD Education Collaboration Task 2 “Structural Integrity Monitoring of UAV Composite Wings”.

6. REFERENCES
1. Staszewski W., Boller C., Tomlison G. (2004), Health Monitoring of Aerospace Structures, Wiley and Sons, West Sussex, England.
2. Goetschel D.B., Dong S.B., Muki R. (1982), “A Global Local Finite Element Analysis of Axisymmetric Scattering of Elastic Waves,” Transactions of the ASME, Vol. 49, pp. 816-820.

3. Al-Nassar Y.N., Datta S.K., Shah A.H. (1991), “Scattering of Lamb Waves by a Normal Rectangular Strip Weldment,” Ultrasonics, Vol. 29, pp. 125-132.

4. Rattanawangcharoen N., Zhuang W., Shah A.H., Datta S.K. (1997), “Axisymmetric Guided Waves in Jointed Laminated Cylinders,” Journal of Engineering Mechanics, Vol. 123, pp. 1020-1026.

5. Chang Z., Mal A.K. (1995), “A Global Local Method for Wave Propagation Across a Lap Joint,” Numerical Methods in Structural Mechanics ASME, Vol. 204, pp. 1-11.

6. Mal A.K., Chang Z. (2000), “A Semi-Numerical Method for Elastic Wave Scattering Calculations,” International Journal of Geophysics, Vol. 143, pp. 328-334.

7. Mal A.K., Chang Z. (1999), “Scattering of Lamb Waves from a Rivet Hole with Edge Cracks,” Mechanics of Materials, Vol. 31, pp. 197-204.
8. Gopalakrishnan S., Doyle J.F., (1995), "Spectral super elements for wave propagation in structures with local non-uniformities," Computer Methods in Applied Mechanics and Engineering, Vol. 121, pp. 77-90.

9. Doyle J.F., (1995), "Determining the size and location of transverse cracks in beams," Experimental Mechanics, Vol. 35(3), pp. 272-280
10. Bartoli I., Marzani A., Lanza di Scalea F., Viola E. (2006). “Modeling Wave Propagation in Damped Waveguides of Arbitrary Cross-section,” J. of Sound and Vibration, Vol. 295, pp. 685-707.
11. Hayashi T., Song W.J., Rose, J.L. (2003), “Guided Wave Dispersion Curves for a Bar with an Arbitrary Cross-section: A Rod and Rail Example,” Ultrasonics, Vol. 41, pp. 175-183.
12. Treyssede F., (2008), "Elastic waves in helical waveguides," Wave Motion, Vol. 45(4), pp. 457-470.

13. Castaings M., Lowe M., (2008), "Finite element model for waves guided along solid systems of arbitrary section coupled to infinite solid media," J.of Acoustical Society of America, Vol. 123(2), pp. 696-708.

14. Hayashi T., Tamayama C., Murase M., (2006), "Wave structure analysis of guided waves in a bar with an arbitrary cross-section," Ultrasonic, Vol. 44(1), pp. 17-24

15. Al-Qahtani H.M., Dutta S.K., Mukdadi O.M., (2005), "Laser-generated thermoelastic waves in an anisotropic infinite plate: FEM analysis," J. of Thermal Stresses, Vol. 28(11), pp. 1099-1122.

16. di Scalea F.L., Matt H., Bartoli I., Coccia S., Park G., Farrar C., (2007), "Health monitoring of UAV wing skin-to-spar joints using guided waves and macro fiber composite transducers," J. of Intelligent Material Systems and Structures, Vol. 18(4), pp. 373-388.
17. Matt H., Bartoli I., de Scalea F.L., (20005), "Ultrasonic guided wave monitoring of composite wing skin-to-spar bonded joints in aerospace structures," J. of Acoustical Society of America, Vol. 118(4), pp. 2240-2252.

18. Sabra K., Srivastava A., Lanza di Scalea F., Bartoli I., Rizzo, P., Conti, S., (2008), “Structural Health Monitoring by Extraction of Coherent Guided Waves from Diffuse Fields,” J. of the Acoustical Society of America, Vol. 123, pp. EL8-EL13.







(5b)





(5a)





(20)





(11)





(8)





(7)








(13a)





(6a)





(6b)





(9a)








(4)





(3)





(2)





(1)





(13d)





(13c)





(13b)





(14)




















A0





A0





 S0





 S0





(16)





(b)





(18)





(a)








 (c)





 (b)





 (a)





(12)





(10)





(9c)





(9b)





(13e)





(13f)





(15)





(17)





(19)





 (a)





 (b)





 (c)





 (c)





 (b)





 (a)








_1291037266.unknown

_1291037841.unknown

_1291038504.unknown

_1291038676.unknown

_1291038776.unknown

_1291038876.unknown

_1291392927.unknown

_1291450535.unknown

_1291039138.unknown

_1291038807.unknown

_1291038719.unknown

_1291038631.unknown

_1291038651.unknown

_1291038576.unknown

_1291038181.unknown

_1291038374.unknown

_1291038440.unknown

_1291038292.unknown

_1291037995.unknown

_1291038047.unknown

_1291037925.unknown

_1291037554.unknown

_1291037745.unknown

_1291037794.unknown

_1291037812.unknown

_1291037775.unknown

_1291037670.unknown

_1291037680.unknown

_1291037425.unknown

_1291037472.unknown

_1291037496.unknown

_1291037518.unknown

_1291037459.unknown

_1291037336.unknown

_1291037378.unknown

_1291037283.unknown

_1291028158.unknown

_1291036208.unknown

_1291037123.unknown

_1291037224.unknown

_1291037254.unknown

_1291037154.unknown

_1291037084.unknown

_1291037100.unknown

_1291037028.unknown

_1291036253.unknown

_1291032512.unknown

_1291032617.unknown

_1291032649.unknown

_1291033262.unknown

_1291032578.unknown

_1291032043.unknown

_1291032405.unknown

_1291031964.unknown

_1291028366.unknown

_1291027476.unknown

_1291027553.unknown

_1291027913.unknown

_1291027513.unknown

_1291026042.unknown

_1291026575.unknown

_1291025807.unknown

